## Slide 1: GE298: Manufacturing Automation Week-1
Class-2: Casting

## Slide 2: Casting
Introduction of molten metal into a mold cavity where the metal confirms to the shape of the cavity
Intricate shapes in a single piece
Internal cavities
Very small and hollow parts can be produced
Important factors in casting operations
Solidification
Molten metal into metal cavity
Heat transfer during solidification and cooling of the metal in the mold
Influence of the type of the mold material
Questions from SME Videos?

## Slide 3: Ingot casting and Continuous Casting
Ingots: First solid form of raw Ingots are used for forging , further material casting etc.
Ingots are passed into Ingot mold.
Squares, Rectangular, circular cross sections
Ferrous Ingots
Oxygen present in the molten metal is rejected out of the casting when the casting when temperature drops
Oxygen combines with carbon to form carbon monoxide causes porosity
Killed steel
Add Aluminum or silicon to form oxides, which deoxidizes the metal, causes shrinkage cavities, lot of scrap.

## Slide 4
Semi Killed steel
Partially deoxidized, some porosity, Economical
Rimmed steel
Lots of blowholes, Usually low carbon steel (0.15% Carbon)

## Slide 5
Expendable casting/Permanent mold Casting
Sand, Plaster, Ceramics
Usually refractories which withstand high temperature of molten metal.
Sand casting
SiO2 -> Silica sand
Naturally bonded, synthetic ( lake sand)
Factors: Fine round grains, good permeability, allows gases to go out.
Types of sand molds
Green Sand | Cold box | No bake molds
Moist/damp skin Dried/over dried | Organic and Inorganic Binder | Synthetic resin with sand

## Slide 6: Various features of a sand mold
Open riser
Vent
Pouring basin(cup)
Flask
Sand
Parting line
Sand
gate
choke
Runner
Mold Cavity
Drag
Cope
Blind Riser
Core Sand

## Slide 7: Patterns
Patterns are made in the shape of the casting
Pattern Materials: Wood, Plastic or metal.
Size, shape, dimensional accuracy, number of components.
Parting agents.
One piece or multiple piece pattern

## Slide 8: A typical match plate pattern used in sand casting
plate
Drag side
Cope side

## Slide 9: Pattern Allowances
Shrinkage Allowance
Patterns are made larger than the casting to compensate contraction of the liquid while freezing.
For internal cavities the allowances should be negative.
If a is the coefficient of thermal expansion, l is the dimension of the casting then the shrinkage allowance will be
a |(q- q o)|

## Slide 10: Cores
Cores
Cores are used to create internal cavities.
Should have similar properties as the mold.
Shaken out after finished casting is produced.
Core Print,Chaplets
Core Boxes

## Slide 11: Design of Casting
Riser - location
Corners, angles and sections
No sharp corners, angles or fillets
  cracking, tearing during solidification
Too large fillet radius?
Smooth sections
Flat areas
Parting lines

## Slide 12
Machining Allowance
Allowance required to remove the rough cast surface. 2 to 25 mm (0.1 to 1’)
Draft Allowance
To facilitate ease of removal, usually ½ to 2 deg.
Shrinkage allowance
Normal shrinkage: Cast iron 0.83 to 1.3%
Aluminum - 1.3%

## Slide 13: Plaster Mold Casting
Plaster of Paris( Calcium Sulfate, Gypsum) + silica flour
The mixture is poured over the pattern (instead of sand)
POP has low permeability, gases cannot escape
Antioch process : Dehydrate & Rehydrate
Usually used for low temperature alloys like aluminum,brass etc. ( metal with melting point below 2000 F)
Components: gears, valves, tooling, ornaments
High precision process.

## Slide 14: Ceramic Mold Casting
Similar to plaster mold. Ceramic slurry
Mixture of fine grained Zircon (ZrSi04), aluminum oxide and fused
Shell is baked at high temperature
Uses
High temp alloys, expensive process
Parts
Stainless Steel or tool steel parts
Examples
Impellers,cutters,dies etc.

## Slide 15: Evaporative pattern casting
Lost Pattern Casting
Polystyrene pattern
Evaporates when it comes in contact with molten metal
Process
Polystyrene beads are placed in preheated die, usually aluminum die.The polystyrene expands and fills die cavity.Again heated to fuse the beads.

## Slide 16: Investment Casting
Lost wax process: 4000,3000 BC
Patterns are made of wax,urea,plastic.
Shell = Silica & binder, ethyl silicate binder & acids, Zircon flour
Intricate shape, precision parts
High temperature process.
Parts: Aircraft components, gears, cams, valves, jewelry.
Molten metal is passed in vacuum to reduce oxidation, isostatic pressure is applied to reduce micro porosity ( 15 ksi pressure at 900 def F)

## Slide 17: Schematic illustration of Investment casting
Mold to make pattern
Wax pattern
Molten metal
Injecting wax or plastic pattern
Ejecting pattern
Pattern assembly (tree)
Slurry coating
Stucco coating
Completed mold
Pattern meltout
Pouring
Shakeout
pattern
casting
Castings by this method cab be made with very fine detail and from variety of materials

## Slide 18: Permanent Mold Casting
Metal mold - permanent
  Pre-Heated dies
  Water cooled
  Good surface finish - good for automation
  Piston, Cylinder heads, connecting rods etc

## Slide 19
Pressure Casting
Pressure applied while filling the casting
Die Casting
Permanent mold method
  Hot Chamber
  Cold Chamber

## Slide 20: Low pressure casting
Graphite mold
Railroad wheel
Air pressure
Molten metal
ladle
Airtight chamber
Refractory tube

## Slide 21: Hot chamber Die casting
Hydraulic shot cylinder
Plunger rod
plunger
Molten metal
pot
Goose neck
Die cavity
2000 psi

## Slide 22: Cold Chamber die casting
ladle
Hydraulic cylinder
Shot sleeve
Plunger rod
Stationary die half
Ejector box
Ejector platen
(Moves)
Stationary platen
Ejector die half
3 to 10 Ksi
in the range of 5000 psi
Sequence of operations in die casting of part in the cold chamber process

## Slide 23: Various types of die casting dies
Single cavity die
Multiple cavity die
Combination die
Unit die

## Slide 24
Centrifugal Casting