## Slide 1
Nanoscience Fundamentals:
Quantum Size Confinement -
Semiconductor Quantum Dots (QDs)
University of Illinois at Urbana-Champaign
Department of Bioengineering
Cancer Nanotechnology
Spring2019
BIOE 479 / 598
Instructor: Prof. Shuming Nie
Notes: What are QDs and what are they used for
Nanocrystals composed of semiconductors
Fluorescent
2. Nie group first of 2
3. Used throughout biology in situations where dyes and proteins have been used
3. Major advantage for molecular scale imaging dynamic
Main benefit: single molecule imaging in cells
Top-down vs bottom up

## Slide 2
Size-Tunable Light Emission
Ten distinguishable emission colors of ZnS-capped CdSe QDs from blue to red excited with a near-UV lamp.
M.Y. Han, X. Gao, & S. Nie, Nature Biotechnology. 19, 631-635 (2001).

## Slide 3
Luminescent Quantum Dots for In-Vivo Imaging and Targeting

## Slide 4: New Sciences on the Nanometer Scale
Bulk Material Nanoparticles Atoms/Molecules

## Slide 5
Quantum Dot Physics
Eg = Bandgap Energy

## Slide 6
Quantum Dot Physics
Quantum confinement effect: Semiconductor particles smaller than the Bohr exciton will demonstrate an increase in the bandgap energy, in accord with the Heisenberg uncertainty principle.

## Slide 7
Core-Shell Quantum Dots

## Slide 8
Shape Control and Surface Passivation

## Slide 9
Size-Tunable QDs (Binary)
Composition-Tunable QDs (Ternary)
Strain-Tunable QDs (Core Shell)

## Slide 10
Bandgap Engineering

## Slide 11
Binary CdSe Dots – Size Tunability

## Slide 12
Ternary CdSeTe Dots: Alloy Composition Tuning
Bailey and Nie, JACS 2003

## Slide 13
Strain-Tunable Quantum Dots
Smith and Nie, Nature Nano, January 2009.

## Slide 14
Bioconjugated Quantum Dots
Quantum dots (QDs): Nanometer-sized semiconductors
Size & material dependent optical properties
High surface/volume ratio
Biological labeling: Colorful tags of biomolecules with highly luminescent QDs
Unique Optical Properties: A superior substitute for organic dyes
Quantum Dots
Meet Biomolecules
A. P. Alivisatos et al., Science 281, 2013-2016 (1998).
S. Nie et. al., Science 281, 2016-2018 (1998).

## Slide 15: Quantum Dot Probes with Proton-Sponge Coating

## Slide 16
Smith and Nie, JACS 2008

## Slide 17: Size-Minimization of QDs

## Slide 18: New Tagging Strategies

## Slide 19: New Delivery Methods

## Slide 20: Dynamic Imaging of Cellular Events

## Slide 21: Intracellular Imaging and Tracking

## Slide 22: Cancer Molecular Profiling with QDs
Her2 Staining/Cancer Cells
Left: Archived (FFPE) Clinical Prostate Tumor Specimen Stained for EGR- and p53

## Slide 23
Direct Mapping of Tumor Heterogeneity on Human Prostatectomy Specimens
IHC
QDs

## Slide 24
Molecular and Cellular Mapping on Surigical Tissue Specimens

## Slide 25
Detection and Identification of Single Malignant Tumor Cells on Prostatectomy Tissue Specimens

## Slide 26
Complex and Suspicious Histopathological Loci – Comparison of H&E and QD Staining

## Slide 27
Multiplexed Detection of Rare Tumor Cells in Hodgkin’s Lymphoma: Hodgkin’s and Reed-Sternberg Malignant Cells (HRS)

## Slide 28
Multiplexed Detection of Rare Tumor Cells in Hodgkin’s Lymphoma: Hodgkin’s and Reed-Sternberg Malignant Cells (HRS)

## Slide 29
Immunofluorescence images of human breast cancer cells (BT-474) labeled with green quantum dots
Gao and Nie, 2003