## Slide 1
Lecture 20: Solids – Metals, Insulators, and Semiconductors
Notes: Kruse qmbands
Interference filter demo
Thermometer demo.
TV “remote” demo (with video camera)
Bare laser
Hi-Tc (maybe)

## Slide 2: Today
Electron energy bands in Solids States in atoms with many electrons – filled according to the Pauli exclusion principle
Why do some solids conduct – others do not – others are intermediate
  Metals, Insulators and Semiconductors
  Understood in terms of Energy Bands and the Exclusion Principle
Solid-state semiconductor devices
  The electronic states in semiconductors
  Transistors, . . .
Superconductivity
  Electrical conduction with zero resistance!
  All the electrons in a metal cooperate to form a single quantum state

## Slide 3: Electron states in a crystal (1)
Again start with a simple atomic state:
+e
r
n = 1
A
Bring N atoms together to form a 1-d crystal (a periodic lattice).
N atomic states  N crystal states.
What do these crystal states look like?
Like molecular bonding, the total wave function is (approximately) just a superposition of 1-atom orbitals.

## Slide 5: Electron states in a crystal (2)
The lowest energy combination is just the sum of the atomic states. This is a generalization of the 2-atom bonding state.
The highest energy state is the one where every adjacent pair of atoms has a minus sign:
There are N states, with energies lying between these extremes.
No nodes! Lowest energy.
N-1 nodes! Highest energy.
Notes: Kruse Energy Bands: qmbands

## Slide 6: Energy Band Wave Functions
FYI: These states are called “Bloch states” after Felix Bloch who derived the mathematical form in 1929. They can be written as: where u is an atomic-like function and the exponential is a convenient way to represent both sin and cos functions
3
1
2
4
5
6
Energy
Lowest energy wave function
Highest energy wavefunction
Closely spaced energy levels form a “band” – a continuum of energies between the max and min energies
Example with six atoms  six crystal wave functions in each band.
Notes: periodic lattice – electrons can travel like free particles.
defects, or no lattice – electrons don’t travel well (e.g., steel, wood…)

## Slide 7: Energy Bands and Band Gaps
In a crystal the number of atoms is very large and the states approach a continuum of energies between the lowest and highest  a “band” of energies. A band has exactly enough states to hold 2 electrons per atom (spin up and spin down).
Each 1-atom state leads to an energy band. A crystal has multiple energy bands. Band gaps (regions of disallowed energies) lie between the bands.
1s band
2s band
Band gap
Notes: Kruse qmbands

## Slide 9: Bands and Band Gaps Occur for all Types of Waves in Periodic Systems
Electron in a crystal – a periodic array of atoms
Energy Bands
Band Gap: no states
Light propagating through a periodic set of layers with different index of refraction – an interference filter
Photon
Transmitted?
Reflected?
Alternating index n1 and n2
Notes: Kruse qmbands

## Slide 10: Interference Filter
Light propagating through a periodic set of layers with alternating index of refraction.
The behavior light waves in this material is the same as that of electron waves in a string of square wells.
For certain wavelengths there is complete reflection, because that wavelength cannot exist inside the material. This is a “stop band”.
For other wavelengths there is complete transmission.
This is a “pass band”.
Photon
Transmitted?
Reflected?
Alternating index n1 and n2

## Slide 11: Interference Filter
Conventional (dye) filters absorb unwanted colors. Interference filters do not absorb light (do not get hot) and are used in many applications: TV, photography, astronomy, … Examples: Red, Green, Blue (RGB)  Yellow, Cyan, Magenta
What is magenta? Answer: Magenta = Red + Blue (no Green)
A magenta filter must have a stop band in the green, but pass red and blue:
Demonstration with a commercial interference filter
Notes: DEMO

## Slide 13: Electrical Conductivity
The ability to conduct electricity varies enormously between different types of solids.
Resistivity  is defined by:
where J = current density and E = applied electric field.
Resistivity depends on the scattering time for electrons.
Resistivity depends on the number of free electrons.
Example properties at room temperature:
Material Resistivity Carrier Type (-m) Density (cm-3)
Cu 2x10-8 1023 conductor
Si 3x103 1010 semiconductor
Diamond 2x1016 small insulator
Notes: The previous slide showed that unless we have a periodic lattice, the electron won’t flow like a free particle.
But even if we DO have a lattice, some materials are still metals, semiconductors or insulators, depending on how many free carriers there are. This requires a quantum description (using Pauli Exclusion principle to fill the bands).

## Slide 14
Why Some Solids Conduct Current and Others Don’t
Conductors, semiconductors, and insulators: Their description is provided in terms of:  Energy Bands for electrons in solids  The Pauli exclusion principle In order for a material to conduct electricity, it must be possible to get the electrons moving (i.e., give them some energy).

## Slide 15: Insulators, Semiconductors and Metals
Energy bands and the gaps between them determine the conductivity and other properties of solids.
Insulators Have a full valence band and a large energy gap (a few eV). Higher energy states are not available.
Semiconductors Are insulators at T = 0. Have a small energy gap (~1 eV) between valence and conduction bands. Higher energy states become available (due to kT) as T increases.
Metals Have a partly filled band. Higher energy states are available, even at T = 0.
E
metals
insulators
semi-
conductors
Valence band
Conduction band
In order to conduct, an electron must have an available state at higher energy.

## Slide 17: Act 1
Consider a crystalline solid in which each atom contributes some electrons to the 3s band. Which situation can produce a conductor.
a. Each atom contributes one 3s electron. b. Each atom contributes two 3s electrons. c. Each atom contributes three 3s electrons.
3s band
3p band
Band gap

## Slide 18: Conductivity of Metals
Sodium: Z = 11 (1s22s22p63s1)
N states
4N states
N states
1s
2s, 2p
3s
The 2s and 2p bands overlap.
Since there is only one electron in the n = 3 shell, we don’t need to consider the 3p or 3d bands, which partially overlap the 3s band.
Atomic states
Fill the bands with 11N electrons.
Each state can hold 2 electrons
Notes: Question: The higher energy bands are broader. Why?

## Slide 19: Conductivity of Metals
Sodium: Z = 11 (1s22s22p63s1)
N states
4N states
N states
1s
2s, 2p
3s
The 3s band is only half filled (N states and N electrons)
These electrons are easily promoted to higher states. Na is a good conductor.
Partially filled band  good conductor
Total # atoms = N Total # electrons = 11N
8N electrons fill this band
2N electrons fill this band

## Slide 21: Semi-classical Picture of Conduction
n = # free electrons/volume  = time between scattering events
J = current density = I/A
F = force = -eE
a = acceleration = F/m
Metal: scattering time gets shorter with increasing T
Temperature, T
Resistivity
Wire with cross section A
e-
E
A more accurate description requires that we treat the electron as a quantum mechanical object.
Notes: Demo with inductor and ohmeter

## Slide 22: Superconductivity
1911: Kamerlingh-Onnes discovered that some metals at low temperature become perfect conductors. The resistance was lower than could be measured (still true today!).
1933: Meissner discovered that superconductors expel a magnetic field. They can be levitated by the magnetic repulsion.
Temperature
Resistivity
Zero!
Demo
The physics in a (small) nutshell:
At low temperatures, the electrons in some materials (e.g., lead) develop an energy gap (not the band gap). This gap makes it impossible for electrons to scatter from impurities, because no states are available.
This does not happen in a superconductor.
Notes: DEMO: Hi Tc levitation

## Slide 23: Applications of Superconductivity
To date, applications have mostly been specialized. In particular, it is much cheaper to operate high field (high current) electromagnets if the wire is superconducting.
Superconducting Quantum Interference Devices (SQUIDs) are also used to make very sensitive magnetic field measurements (e.g., to make part in 1012 measurements of magnetic susceptibility).
MRI
LHC accelerator
http://rich.phekda.org/squid/technical/part4.html
The holy grail of SC technology is electrical power distribution (7% is lost in the power grid). This is one reason HiTc superconductors are important, but it’s not yet competitive.
http://www.nano-opt.jp/en/superconductor.html

## Slide 25: Semiconductors
The electrons in a filled band cannot contribute to conduction, because with reasonable E fields they cannot be promoted to a higher kinetic energy. Therefore, at T = 0, pure semiconductors are actually insulators.
Energy Gap Egap ≈ 1.1 eV
Filled band at T = 0 (Valence band)
Empty band at T = 0. (Conduction Band)
Notes: DEMO: Fever thermometer.

## Slide 26: Act 2
Consider electrons in a semiconductor, e.g., silicon. In a perfect crystal at T = 0 the valence bands are filled and the conduction bands are empty  no conduction. Which of the following could be done to make the material conductive?
a. heat the material
b. shine light on it
c. add foreign atoms that change the number of electrons

## Slide 27: Semiconductors
The electrons in a filled band cannot contribute to conduction, because with reasonable E fields they cannot be promoted to a higher kinetic energy. Therefore, at T = 0, pure semiconductors are actually insulators.
At higher temperatures, however, some electrons can be thermally promoted into the conduction band.
Metal: scattering time  gets shorter with increasing T
Temperature, T
Resistivity
Semiconductor: number n of free electrons increases rapidly with T (much faster than  decreases)
Energy Gap Egap ≈ 1.1 eV
Filled band at T = 0 (Valence band)
Empty band at T = 0. (Conduction Band)
This graph only shows trends. A semiconductor has much higher resistance than a metal.
Notes: DEMO: Fever thermometer.

## Slide 29: Digital Thermometers
Digital thermometers use a thermistor, a semiconductor device that takes advantage of the exponential temperature dependence of a semiconductor’s resistance. As the temperature increases, the resistance of the material drops markedly and can be used to determine the temperature.
Notes: DEMO: Digital thermometer guts.

## Slide 30: Semiconductors
Silicon: Z = 14 (1s22s22p63s23p2)
4N states
4N states
N states
1s
2s, 2p
3s, 3p
The 3s/3p band is only half filled (4N states and 4N electrons)
Total # atoms = N
Total # electrons = 14N
8N electrons fill this band
2N electrons fill this band
Why isn’t Silicon a metallic
conductor, like sodium?