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TRANS-IPIC Quarterly Progress:

Project Description:

Research Plan - Statement of Problem

Unbonded post-tensioning (PT) is widely used in segmental construction and spliced girders, particularly for long-span bridges [1-3]. As the strands are external or placed in ducts without grouting, they remain accessible during a bridge’s service life, enabling inspection, evaluation, and replacement if needed. However, the lack of bond between the strands and the concrete reduces structural efficiency. The capacity of an unbonded PT girder is typically controlled by concrete crushing or by fracture of the bonded reinforcement rather than by yielding of the PT strands, resulting in a lower capacity than that of bonded systems. Thus, unbonded PT sacrifices some structural capacity in exchange for improved serviceability, durability, and constructability. In this project, we propose replacing conventional concrete (CC) with ductile fiber-reinforced concrete, known as an Engineered Cementitious Composite (ECC), to enhance the strength and displacement capacity of unbonded PT girders while retaining their durability advantages [4-9]. The distributed microcracking behavior of ECC is more compatible with strand deformation, and numerical analyses indicate that it can improve the structural performance of unbonded PT girders, bringing them closer to the behavior of bonded systems. This work aims to expand the use of unbonded PT in durable, long-lasting bridges.

The specific objectives of this project are as follows:
1. To develop a suitable ECC for use in a prestressed concrete girder
2. To experimentally evaluate the effect of replacing CC with ECC on the flexural behavior of a beam with unbonded PT strands 
3. To develop a numerical model for accurately modeling the behavior of a girder with unbonded PT strands and investigating the girder behavior through parametric analysis 
4. To provide recommendations for designing girders with ECC, accounting for its tensile strength and ductility 

Research Plan - Summary of Project Activities (Tasks)

The following tasks will be performed to achieve the research objective stated above. 

Task 1 - ECC Mix Development: An ECC mix with compressive strength comparable to CC, commonly used in prestressed girders, will be developed. A typical ECC has a compressive strength of about 5-7 ksi. Increasing the compressive strength to our target range, suitable for precast concrete bridge members (8-12 ksi), while achieving a tensile strain capacity of at least 1%, will require modifications to the matrix and the fiber-matrix bond. 

Task 2 - Proof-of-concept testing: To experimentally test the idea of replacing CC with ECC to achieve higher flexural capacity, beam specimens with ECC and CC will be fabricated using unbonded strands. Bending tests will be conducted. Our preliminary numerical analysis showed that having some bonded strands, rather than none, is optimal for leveraging the tensile ductility of ECC. Therefore, some bonded strands will be considered for specimen design. Displacements, strand stresses, reinforcement, and concrete strains will be measured. The outcomes of this task are the load-displacement relationship, crack patterns, and strand stress at failure. 

Task 3 - Numerical model development and validation: A numerical model in a finite-element software will be developed and validated. The model will build on the principles of strain and displacement compatibility (with concrete) for bonded and unbonded reinforcement, respectively. The numerical model will provide load-displacement behavior, as well as stresses and strains in concrete, reinforcing bars, and strands at any section along the girder length to develop a deeper understanding of the structural behavior of girders with unbonded PT strands. The numerical model created in Task 3 will be validated using the data collected in Task 2. 

Task 4 - Parametric studies: The validated models from Task 3 will be used to assess the impact of design parameters on ECC’s effectiveness. The specimens tested in Task 2 will be modeled with varying total reinforcement areas, two concrete types, and bonded strands to total reinforcement ratios. 

Task 5 - Design method development: The nominal moment capacity (Mn) and the stress in unbonded strands at Mn (fps) will be calculated using a conventional mechanics-based force-equilibrium approach commonly used for CC design. However, unlike the CC design, which assumes zero tensile strength of CC, ECC’s tensile strength will be considered in the design.

Project Progress:

Progress for each task

Task 1 – ECC Mix Development (100% complete):

Task 1 focused on developing an ECC mix with compressive strength comparable to that of conventional concrete (CC) typically used in prestressed concrete girders. To develop such a mixture, the first step was to prepare trial mixtures to increase the matrix compressive strength. Four trial mixtures with weight proportions shown in Table 1 were developed. Details related to trial mixture selection and the mixing procedure were provided in the Q1 report.

Table 1. Mixture composition and strength qualification test results
	Mixture ID
	Cem-ent
	Fly ash
	Silica-sand
	Water/
Binderratio*
	HRWRA
	Micro-silica
(955U)
	PVA fibers (Vol %)
	4-day comp. strength, ksi 
	COV (%)

	Mix 1
	1
	1.20
	0.82
	0.31
	1.00%
	-
	2%
	3.7
	4.7

	Mix 2
	0.95
	1.30
	0.86
	0.31
	1.33%
	0.05
	2%
	3.2
	6.9

	Mix 3
	0.85
	1.41
	0.97
	0.31
	1.00%
	0.15
	2%
	3.5
	5.4

	Mix 4
	1
	1.20
	0.82
	0.24
	1.66%
	-
	2%
	5.5
	4.3


* Binder includes cement and supplementary cementitious materials – fly ash and microsilica 

Among the four mixtures in Table 1, Mix 4 exhibited the highest 4-day compressive strength. However, the fresh properties and dispersion of PVA fibers in Mix 4, which are critical to achieving tensile ductility, were unsatisfactory. Therefore, the second step aimed to achieve the desired tensile ductility (>1%) by replacing the PVA fibers with high-molecular-weight polyethylene (PE) fibers in Mix 4. Compared with hydrophilic PVA fibers, PE fibers are hydrophobic and therefore exhibit lower water demand. The PE fibers also allow greater slip at the fiber-matrix interface than PVA fibers, resulting in high complementary energy sufficient to overcome the fracture energy barrier for achieving multiple micro-cracking under tension.

The resulting ECC mixture exhibited the following mechanical properties after 28 days of curing under ambient conditions:

· Compressive strength of 2” cube (ASTM C109) [10] = 9.6 ksi (COV= 5%)
· Compressive strength of 3” cylinders (ASTM C39) [11] = 7.3 ksi (COV = 12%)
· Tensile strength [12] = 0.8 ksi (COV = 16%)
· Cracking strength [12] = 0.6 ksi (COV = 23%)
· Tensile strain capacity [12] = 2.1% (COV = 27%)

Task 2- Proof of concept testing (55% complete):

Task 2 focused on experimentally evaluating the concept of replacing conventional concrete (CC) with engineered cementitious composite (ECC) to achieve higher flexural capacity in prestressed concrete beams. 

Conventional concrete mix design (Complete):
For a comparative evaluation of the ECC and CC beams, a conventional concrete mixture with a compressive strength comparable to that of ECC (developed in Task 1) was designed. The developed CC mixture consisted of crushed limestone aggregates, river sand, tap water, and a high-range water-reducing admixture (HRWRA). The mixture was proportioned to achieve a target compressive strength of approximately 8 ksi at 28 days, consistent with the 28-day strength of the ECC developed in Task 1. The observed compressive strengths of CC under ambient curing conditions are as follows:

· 7-day compressive strength of 3” cubes (ASTM C39) [11] = 7.6 ksi (COV= 6%)
· 28-day compressive strength of 3”×6” cylinder (ASTM C39) [11] = 8.8 ksi (COV = 4%) 

Beam cross-section design (Complete):

Trial beam cross-sections, reinforcement detailing, and prestressing configurations for the planned proof-of-concept testing were evaluated. These designs considered the available testing facilities in the PI’s laboratory and the measurement requirements necessary to capture the structural response and outcomes relevant to the project objectives. Based on these considerations, the following two sets of beam cross-sections are planned for evaluation:
 
· Set 1 - Post-tensioned beams with ordinary reinforcement: This set will consist of two beams, one with conventional concrete as a control specimen and another with ECC. These beams consist of one 0.5” diameter post-tensioned strand with estimated prestress after losses of 60 ksi and one #6 rebar in the tension zone. Sufficient lateral reinforcement is provided to avoid shear failure.
· Set 2 - Post-tensioned beams with prestressing strand: This set also consists of two beams, one with conventional concrete and another with ECC. These beams consist of two 0.5” diameter strands, one post-tensioned and one pretensioned, creating a hybrid prestressing system. No additional reinforcement is provided in longitudinal directions. Sufficient lateral reinforcement is provided to avoid shear failure.

Beams in both sets have a cross-section of 6” wide and 10” deep, and the total length of the beams is 10 feet.

Beam fabrication (50%):

Fabrication of the first set of beams is complete. Fabrication of the second set of beams is in progress. Figure 1 shows the rebar frame, a cast beam, and accompanying material-scale specimens for quality control. This task will be completed in Q3 of the project.
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Figure 1 (a) Rebar frame, (b) Cast beam, (c) Material-scale specimens 

Task 3 - Numerical model development and validation (50% complete):

A numerical model for simulating hybrid post-tensioned beams was developed for both sets of beams designed in Task 2. The beams include – (1) Hybrid post-tensioned and pretensioned conventional concrete beam (CC prestress), (2) Hybrid post-tensioned and pretensioned ECC beam (ECC prestress), (3) Post-tensioned conventional concrete beam with ordinary reinforcement (CC RF), and (4) Post-tensioned ECC beam with ordinary reinforcement (ECC RF). The model was first validated against analytical calculations for longitudinal stresses at various beam depths and for camber under applied prestress loads. Upon validation, the model was used to estimate the load-deflection behavior of the four beams in Task 2 under 4-point loading, as shown in Figure 2. The numerical model will be further calibrated to capture the observed load-deflection behavior following the beams' testing in Task 2.
[image: ]
Figure 2. Load deflection behavior of different hybrid-post-tensioned beams
Remaining tasks have not yet started

Percent of research project completed
50%

Expected progress for next quarter
In the next quarter, Tasks 2 and 3 will be completed, and Task 4 will be in advanced stages

Educational outreach and workforce development

Accepted Students Day (ASD) 

[bookmark: _Hlk193452349][bookmark: _Hlk193448357]Location- Department of Civil, Structural, and Environmental Engineering (CSEE), University at Buffalo (UB), Buffalo, New York.
Date- April 11, 2026 and April 26, 2026
Details- Students who have been offered admission to UB in Fall 2026 visited the Department of Civil, Structural and Environmental Engineering (CSEE) with their family and friends. They interacted with TRANS-IPIC-associated faculty and students and got acquainted with ongoing research activities supported by TRANS-IPIC. 
[image: ] [image: ]
TRANS-IPIC-associated PhD student demonstrating TRANS-IPIC-supported research to accepted students for fall 2026 and their families.

Technology Transfer
None



Research Contributions:

Papers that include TRANS-IPIC UTC in the acknowledgments section:
None

Presentations and Posters of TRANS-IPIC funded research:
None

Please list any other events or activities that highlights the work of TRANS-IPIC occurring at your university (please include any pictures or figures you may have). Similarly, please list any references to TRANS-IPIC in the news or interviews from your research. 
None


Appendix 1: 

Research Activities, leadership, and awards (cumulative, since the start of the project):

A. Number of presentations at academic and industry conferences and workshops of UTC findings
· No. = 0

B. Number of peer-reviewed publications submitted based on outcomes of UTC funded projects
· No. = 0

C. Number of peer-reviewed journal articles published by faculty.
· No. = 2

D. Number of peer-reviewed conference papers published by faculty.
· No. = 1

E. Number of TRANS-IPIC sponsored thesis or dissertations at the MS and PhD levels.
· No. MS thesis = 0
· No. PhD dissertations = 0
· No. citations of each of the above = 0

F. Number of research tools (lab equipment, models, software, test processes, etc.) developed as part of TRANS-IPIC sponsored research
· None

G. Number of transportation-related professional and service organization committees that TRANS-IPIC faculty researchers participate in or lead.
· Professional societies
· No. participated in = 4
· No. lead = 0
· Advisory committees (No. participated in & No. led)
· No. participated in = 2
· No. lead = 0
· Conference Organizing Committees (No. participated in & No. led)
· No. participated in = 2
· No. lead = 0
· Editorial board of journals (No. participated in & No. led)
· No. participated in = 2
· No. lead = 0
· TRB committees (No. participated in & No. led)
· No. participated in = 1
· No. lead = 0

H. Number of relevant awards received during the grant year
· No. awards received = 0

I. Number of transportation-related classes developed or modified as a result of TRANS-IPIC funding.
· No. Undergraduate = 0
· No. Graduate = 2

J. Number of internships and full-time positions secured in the industry and government during the grant year.
· No. of internships = 0
· No. of full-time positions = 0
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